Abstract

Introduction: There is low incidence of trauma in posterior teeth, and their complications are rarely reported in the literature. This report describes a case of internal root resorption with communication with the periodontal area as a result of traumatic dental injury of a permanent molar tooth.

Materials and methods: The treatment consisted of chemo-mechanical preparation and the use of calcium hydroxide as intracanal medication, followed by filling and sealing of the resorption area with mineral trioxide aggregate.

Results: After 5 years of follow-up, the tooth was in function, without signs or symptoms and the resorption area was repaired.

Conclusion: We emphasize the importance of follow-up in cases of dental trauma, even in cases of low severity, such as subluxative injury, in order to predict possible sequelae ​​in advance. The correct approach to treatment of the ​​resorption area and sealing with mineral trioxide aggregate ensured the successful outcome of the case.

Key Words: molar, permanent dentition, tooth injuries, root resorption

Introduction

Traumatic dental injury (TDI) in permanent teeth is a common occurrence and there may be a prevalence of approximate 20% [1], with the anterior region being the most affected [2]. Nevertheless the incidence of trauma in posterior teeth is low, and their complications are underreported in the literature [3,4]. The main causes of TDI are falls, collisions and sports practice [3]. However, the risk during sports practice varies according to the type of sport practiced, gender, level of competition and exposure time [5].

TDI may lead to injuries of different severities, which are determined by the force and direction of the impact [6]. As a result of severity of the injury, various sequelae can be expected, such as complications in pulp and periodontal ligament healing which may lead to pulp necrosis, obliteration of the root canal, root resorption and loss of the supporting bone [7]. The prognosis depends on the stage of tooth development, type, severity and combinations of traumatic injuries [8]. Luxation injuries are the most likely to result in root resorption, whereas in cases of concussion and subluxation, this type of complication is less likely to develop [9].

Resorption is a late complication and it is diagnosed by radiographic exam [6]. However, in the early stages, this diagnosis is difficult to make [10]. Therefore, resorption is generally diagnosed at later stages, in which communication between the pulp canal space and periodontal tissues may occur. In such cases, Mineral Trioxide Aggregate (MTA) is considered the material of choice because of its good sealing characteristics and biocompatibility [11]. In addition, it creates a favorable periodontal healing environment, which allows the growth of new cementum on its surface [12].

This report describes a case of internal root resorption with communication with the periodontal area as a result of TDI in a permanent molar tooth, with a successful clinical and radiographic outcome after 5 years of follow-up. To the author’s knowledge, in the literature there are no reported studies that have assessed the long-term complications caused by TDI in posterior teeth.

Case Report

The patient, a 23-year-old man, sought care at the Dental Clinic of an Institution of Higher Education due to sensitivity and sinus tract in the right permanent first molar region. The patient reported a history of trauma about 12 months previously while practicing taekwondo, in which he had experienced tooth loosening and sensitivity to touch. At the time, he sought the care of a health professional, and splinting with orthodontic wire for 15 days and occlusal adjustment were performed. According to the patient's report, there was no subsequent follow-up.

On the clinical examination, there was a small edema and a sinus tract in the buccal region of the first right permanent molar, which was nonvital, as assessed by cold test (Endo Ice, Hygenic Corp., Akron, OH, USA). There was mild sensitivity to palpation and vertical/horizontal percussion. Periodontal probing was considered within normal limits. The radiograph showed an area suggestive of ​​internal root resorption in the middle-cervical third of the mesial buccal (MB) canal, and there was widening in the periodontal ligament space of the first right permanent molar (Figure 1-A). When sinus tracking was performed by inserting a gutta-percha cone, the cone went directly to the apex of the MB root (Figure 1-B). Under local anesthesia and after placement of a rubber dam, access to the pulp chamber of the first right permanent molar was performed. After access, the canals were irrigated with 2.5% sodium hypochlorite, and shaped with the rotary Profile System (Dentsply - Maillefer, Ballaigues, Switzerland). During instrumentation, intense bleeding from the MB canal was observed, probably due to communication with the periodontal tissue. This canal was therefore, irrigated with a solution of calcium hydroxide powder and sterile distilled water. After controlling the bleeding, the canals were dried with sterile paper cones and filled with calcium hydroxide powder mixed to a paste with sterile distilled water (1:1). After 7 days, closure of the sinus tract occurred. The intracanal medication was removed and the MB canal was reshaped with the same protocol used in the first visit. Again some bleeding from the cervical portion of the MB canal was observed. Thus, the canal was refilled with intracanal medication consisting of calcium hydroxide powder mixed to a paste with sterile distilled water (1:1). Ten days later, the tooth showed a negative response to palpation and the percussion test, absence of bleeding and the sinus tract was nonexistent. Then the canals were filled with gutta-percha and Pulp Canal Sealer (SybronEndo, Sybron Dental Specialties Inc, Orange, CA), by means of the continuous wave of condensation technique, using the System B Heat-Source (System B, Analytic Technology, Redmond, USA). However, in the MB canal, in addition to apical sealing with gutta-percha and sealer, the middle and coronal thirds of the canal were sealed with gray MTA (Pro-Root MTA, Dentsply, Tulsa Dental, OK, USA) (Figure 2-A). After endodontic filling, resorption areas were also observed in the palatine canal (Figure 2-B). Immediate coronal sealing was performed with light-cured light polymerized resin and the patient was referred to another professional for prosthetic reconstruction.

Clinical and radiographic examination after 05 years showed no evidence of swelling or sinus tract, the tooth was not sensitive to percussion, and the patient did not report any symptoms. A radiograph showed complete healing of the periradicular area (Figure 2-C).

Discussion

Approximately 11-40% of all sports injuries involve the face. These lesions are more common due to   direct contact with the ball or player-to-player [13]. The most common TDI in sports are crown fractures, soft tissue injuries and subluxations [14]. Despite this high incidence, sports practice as an etiological factor for TDI is higher in school-aged children than in teenagers and young adults [1].

The patient report suggested that the injury suffered by practicing taekwondo was a subluxation, which is characterized as an abnormal loosening of the tooth without its displacement [15], as a result of a lower periodontal ligament impact [16]. The treatment depends on the degree of mobility, and the splint may be indicated in cases of severe mobility [17].

According to the patient’s report, the initial treatment was the placement of an orthodontic wire splint for a period of 15 days. It was not possible to determine whether the splinting used was rigid or semi-rigid, because the first examination was performed by another professional. Rigid splinting can lead to pulp canal obliteration [18], which was not observed in the present case; or to pulp necrosis [19], which occurred in this case and was associated with root resorption. However, a systematic review suggested that prognosis is determined by the type of injury rather than factors associated with the splinting [20].

Internal resorption occurs due to inflammation of the apical pulp tissue caused by the coronal pulp infection and necrosis [21]. However, as verified in this report, the pulp may become non-vital after the resorption period, and an apical inflammation may develop [21]. The diagnosis of resorption was made by radiographic examination, which showed a radiolucent oval shaped enlargement in the root canal space area, characteristic of this type of complication [9,22].

Pulp necrosis is considered the most common dental trauma complication [23,24]. Studies have shown that 13.2 to 16.5% of teeth become necrotic after subluxation [24,25], however internal resorption was found in only 1.9% of the cases [24]. It is important to note that all of these previously mentioned studies examined anterior teeth [16,23,24]. To the author’s knowledge there are no studies that have assessed long-term complications caused by TDI in posterior teeth.

The follow-up of patients with dental trauma is essential. In cases of subluxation, radiographic monitoring is recommended, beginning in the first four weeks and continuing for one year to eliminate the possibility of healing complications occurring [6,15]. However, the majority of pathological injuries are usually diagnosed in the first 3 months [23].

The goal of treatment of teeth with internal resorption is to remove all the blood supply from the canal) [9,22]. Calcium hydroxide was used as an intracanal medication in order to maximize the disinfection of the necrotic tissue in the resorption area, facilitate its removal, prevent the invagination of the tissue into the canal and to reduce bleeding [9,22].

The success of perforation repair depends on an adequate marginal seal between the material and walls of the perforation. In the present case, filling was performed by the continuous heat wave condensation technique with the use of MTA to repair the defect caused by resorption. The choice of MTA was based on its superior properties in terms of biocompatibility and long-term sealing ability [11].

In this study, after five years of follow-up, the tooth was asymptomatic and there was complete healing of the periradicular lesion, demonstrating that the treatment described here was successful. Based on the long term result of the reported case, the MTA proved to be a good option for the treatment of teeth with invasive inflammatory resorption.

References

- Andersson L. Epidemiology of Traumatic Dental Injuries. J Endod 2013 Mar-Apr; 39(2):S2-S5.

- Glendor ULF. Epidemiology of traumatic dental injuries – a 12 year review of the literature. Dent Traumatol 2008 Dec; 24(6):603-611.

- Ajayi DM, Abiodun-Solanke IM, Sulaiman AO, Ekhalufoh EF.  A retrospective study of traumatic injuries to teeth at a Nigerian tertiary hospital. Niger J Clin Pract 2012 Jul-Sep; 15(3):320-325.

- Soares TR, Risso PA, Maia LC. Traumatic dental injury in permanent teeth of young patients attended at the Federal University of Rio de Janeiro, Brazil. Dent Traumatol 2014 Aug; 30(4):312-6.

- Glendor U. Aetiology and risk factors related to traumatic dental injuries – a review of the literature. Dent Traumatol 2009 Feb; 25(1):19-31.

- Andreasen JO, Andreasen FM, Anderson L. In: Textbook and color atlas of traumatic injuries to the teeh. 4th ed. Oxford: UK, Blackwell Munksgaard; 2007.

- Andreasen JO, Ahrensburg SS. History of the Dental Trauma Guide. Dent Traumatol 2012 Oct; 28(5):336-344.

- Lauridsen E, Hermann NV, Gerds TA, Kreiborg S, Andreasen JO. Pattern of traumatic dental injuries in the permanent dentition among children, adolescents, and adults. Dent Traumatol 2012 Oct; 28(5):358-363.

- Trope M. Root Resorption due to Dental Trauma. Endod Topics 2002 Mar; 1(1):79-100.

- Estrela C, Bueno MR, De Alencar AH, Mattar R, Valladares Neto J, Azevedo BC, De Araújo Estrela CR. Method to Evaluate Inflammatory Root Resorption by Using Cone Beam Computed Tomography. J Endod 2009 Nov; 35(11):1491-7.

- Mente J, Leo M, Panagidis D, Saure D, Pfefferle T. Treatment outcome of mineral trioxide aggregate: repair of root perforations-long-term results. J Endod 2014 Jun; 40(6):790-6.

- Holland R, Filho JA, de Souza V, Nery MJ, Bernabé PF, Junior ED. Mineral trioxide aggregate repair of lateral root perforations. J Endod 2001 Apr; 27(4):281-4.

- Saini R. Sports dentistry. Natl J Maxillofac Surg 2011 Jul; 2(2):129-31.

- Sepet E, Aren G, Dogan Onur O, Pinar Erdem A, Kuru S, Tolgay CG, Unal S. Knowledge of sports participants about dental emergency procedures and the use of mouthguards. Dent Traumatol 2014 Oct; 30(5):391-5.

- Diangelis AJ, Andreasen JO, Ebeleseder KA, Kenny DJ, Trope M, Sigurdsson A, Andersson L, Bourguignon C, Flores MT, Hicks ML, Lenzi AR, Malmgren B, Moule AJ, Pohl Y, Tsukiboshi M. International Association of Dental Traumatology guidelines for the management of traumatic dental injuries: 1. Fractures and luxations of permanent teeth. Dent Traumatol 2012 Apr; 28(2):2-12.

- Hermann NV, Lauridsen E, Ahrensburg SS, Gerds TA, Andreasen JO. Periodontal healing complications following concussion and subluxation injuries in the permanent dentition: a longitudinal cohort study. Dent Traumatol 2012 Oct;28(5):386-93.

- Murray JM. Mandible Fractures and Dental Trauma. Emerg Med Clin N Am 2013 May; 31(2):553-573.

- Andreasen FM. Pulpal healing after luxation injuries and root fracture in the permanent dentition. Endod Dent Traumatol 1989 Jun;5(3):111-131.

- Andreasen JO, Andreasen FM, Mejàre I, Cveck M. Healing of 400 intra-alveolar root fractures. 2. Effect of treatment factors such as treatment delay, repositioning, splinting type and period and antibiotics. Dent Traumatol 2004 Aug;20(4):203-11.

- Kahler B, Heithersay GS. An evidence-based appraisal of splinting luxated, avulsed and root-fractured teeth. Dent Traumatol 2008 Feb;24(1):2-10.

- Trope M. Luxation injuries and external root resorption – etiology, treatment and prognosis. J Calif Dent Assoc 2000 Nov;28(11):860-6.

- Haapasalo M, Endal U. Internal inflammatory root resorption: the unknown resorption of the tooth. Endod Topics 2006 Jul;14(1):60-79.

- Soares TR, Luiz RR, Risso PA, Maia LC. Healing complications of traumatized permanent teeth in pediatric patients: a longitudinal study. Int J Paediatr Dent. 2014 Sep;24(5):380-6.

- Hecova H, Tzigkounakis V, Merglova V, Netolicky J. A retrospective study of 889 injured permanent teeth. Dent Traumatol 2010 Dec;26(6):466-75.

- Pugliesi DM, Cunha RF, Delbem AC, Sundefeld ML. Influence of the type of dental trauma on the pulp vitality and the time elapsed until treatment: a study in patients aged 0-3 years. Dent Traumatol 2004 Jun;20(3):139-42.

Figure Legends

Figure 1. (A) Initial radiograph; (B) tracing of the sinus tract.

Figure 2. (A) Apical segment filled and MTA in the mid-cervical third; (B) final filling; (C) radiograph of follow-up 5 years after filling.