May 30th, 2017.

Dr. Sergio Eduardo de Paiva Gonçalves

Editor-in-Chief, Brazilian Dental Science

Dear Dr. Gonçalves,

Firstly, we would like to thank you very much for your comments on our manuscript. We appreciate and consider them for the improvement of the paper.

Enclosed is the revised version of our manuscript entitled “Marginal leakage of temporary restoration after intraradicular post preparation with or without waterproofing”.

We highlighted the changes in the manuscript by using colored text.

Thank you for the opportunity to revise our manuscript. We hope that you and the reviewers will now find it acceptable for publication in the Brazilian Dental Science.

Sincerely,

DDS, Msc, Phd student Leopoldo Cosme Silva

School of Dentistry, Federal University of Alfenas

Rua Gabriel Monteiro da Silva, 700. Alfenas-MG. Brazil. CEP: 37130-000

Phone #: 55 35 3299 1425     Fax #: 55 35 3299 1063

E-mail: leopoldocosme@gmail.com

Manuscript ID 1411: Point-by-point review

1- Has this methodology been validated in any article?

The methodology of dye infiltration is consolidated by the scientific literature. Previous studies have employed similar research methodology.

RAMOS AA, GALAN-JÚNIOR J. Infiltração marginal de cimentos provisórios em dentes tratados endodonticamente. RGO, v. 53, n. 4, p. 305-308. 2004.

FERRAZ EG. et al. Sealing of temporary cements in endodontics. RGO, v. 57, n. 3, p. 323-327, jul./set. 2009.

FERRAZ EG, CARVALH CM, CANGUSSU MCT,  ALBERGARIA S,  PINHEIRO ALB,  MARQUES ABC

TANOMARU-FILHO M, SPINOLA SG, REIS JM, CHAVEZ-ANDRADE GM, GUERREIRO-TANOMARU JM. In vitro sealing ability of temporary restorative materials used in endodontics. Gen Dent. 2009 Nov-Dec; v. 57, n. 6, p. 622-5.

2 – Were those dry teeth?

No. During the experimental period the teeth were maintained in a recipient containing a sponge soaked in water, to ensure humidity. Such information was provided in the manuscript.

3 - 0.5% sodium hypochlorite does not disinfect the tooth, because the percentage of chlorine depends on how it was stored and generally has less than 0.5%

0.5% sodium hypochlorite was initially used for prior disinfection of the teeth to improve the biosafety of the procedure. However, this procedure could have been excluded from the study, since individual protective equipment was also used throughout the experimental period. After this initial procedure the root canals were prepared and cleaned with with copious irrigation using 2.5% NaOCl as it is described in the article.

4- 48 hours in saline solution dehydrates the tooth and consequently changes the result

The teeth were maintained in water for hydration, not in saline solution as described in main document. Such information was corrected in the manuscript in red colored text.

.5. The difference in volume does not mean more or less infiltration. Several factors can interfere with root canal diameter, dentin permeability, tooth age, how much time has been extracted, etc.

In this study, the samples were weighed on a precision scale before and after the dye. Thus, the difference between these two measurements reflects the degree of infiltration of the dye in the samples.

6 - I would like to make a suggestion, you could work with the infiltrated area, I think the result would be more accurate.

We appreciate and consider your suggestion, however the photographic image that would serve as the basis for the infiltrated area count does not allow us to evaluate all the infiltration due to the impossibility of three-dimensional images. Therefore, in the study model used in this study, the dye weight was an alternative found.

Marginal leakage of temporary restoration after intraradicular post preparation with or without waterproofing

Abstract

This study evaluated the leakage volume of 1% Rhodamine B which received or not an internal waterproofing material. The hypothesis is that the waterproofing reduces microleakage. Methods: Forty-two human teeth were selected for this study. After access, preparation, and filling of root canals, the teeth were divided into 3 groups: GI – sealed with Cimpat Blanc®, without intraradicular post/core preparation; GII - sealed with Cimpat Blanc®, with intraradicular post/core preparation, and GIII – sealed with Cimpat Blanc®, with intraradicular post/core preparation and internal waterproofing material with ethyl cyanoacrylate. T-test was used to analyze difference between initial and final weight and there was difference (p<0.05). To analyze infiltration of the colorant, the volume was the comparison variable. Shapiro Wilk- test was applied and showed normal distribution of the variables. ANOVA (p=0.0013 / p<5%) applied and determined a statistical difference between the groups. When comparing the groups together, GIII show the smallest leakage rate when compared with the other groups, being statistically different (Tukey test -p<0.5). In endodontically treated teeth receiving temporary restoration, the use of ethyl cyanoacrylate as internal waterproofing material is effective in preventing microleakage.

Keywords: Dental leakage; Endodontics; Dental restoration, temporary; Coloring agents.

INTRODUCTION

Temporary restoration are sometimes necessary after root canal filling, e.g. between appointments during the prosthesis manufacturing, requiring or not intraradicular post and core. Without a hermetic sealing, bacterial microleakage might occur, leading the endodontic treatment to failure [1-4]. Therefore, ideally, temporary restorative materials should provide a hermetic coronary sealing, thus preventing microleakage [5,6].

This is particularly important when intraradicular post and core are indicated because it requires more than one appointment to be completed [7-9]. Structurally compromised teeth need to receive an intraradicular post and core to restore their function in mouth; however, the time between appointments may lead to salivary and bacterial contamination, which will consequently compromise the cleaning obtained during the endodontic treatment [5,6,10,11]. Thus, some materials (adhesives and cyanoacrylates) have been used to improve the sealing of these cavities [11].

Many studies have assumed that there is a correlation between bacterial penetration and dye penetration, although these methods had not been tested simultaneously with the same samples until nowadays. To analyze the sealing capacity, some dyes (methylene blue, eosin, and Rhodamine B) are used, in vitro, to measure microleakage [12-15]. Researches reported that all restorative materials underwent microleakage [5-7,16]. While others afirmed that the use of waterproofing materials (ethyl cyanoacrylate) associated with temporary restorative materials would decrease the microleakage [17-19].

As, the longevity of provisional restorations is related to, a perfect adaptation and a strong, long-term union between restoration and teeth structures, therefore, evaluation of marginal leakage of provisional restorative materials luted with cements using the standardized procedures is essential. This study aimed to evaluate, in vitro, the leakage of Rhodamine B 1%, in provisional restorations, after intraradicular post preparation with and without internal application of waterproofing material (ethyl cyanoacrylate). The hypothesis of this study is that the waterproofing reduces microleakage

MATERIALS AND METHODS

### This study was submitted and approved by the Institutional Review Board regarding ethical aspects (protocol no. #026/2010). Forty-two teeth single-rooted human maxillary teeth were selected from the teeth bank of the institution, including incisors and canines and maxillary. All teeth were examined at 10X magnification, and those with microcracks were excluded. The teeth were cleaned with running water, immersed in 0.5% sodium hypochlorite solution (NaOCl) (Rioquimica™, São Jose do Rio Preto, SP, Brazil) for 72 hours to desinfect the surface, and immersed in wather for 48 hours for hydration. During the experimental period the teeth were maintained in a recipient containing a sponge soaked in water, to ensure humidity. Subsequently, the endodontic access was performed with spherical diamond drills (KG Soresen™, Cotia, SP, Brazil), at high-speed, under refrigeration. The convenience shape of pulp chamber was obtained using Endo Z drills (Maillefer™, Petropolis, RJ, Brazil).

### The middle and cervical thirds of the root canal were prepared and cleaned using Gates-Glidden size #3 and #4 drills (Denstsply™, Maillefer, Petropolis, RJ, Brazil) and the contents of the apical third were removed using Hedströen and K files (Dentsply™, Maillefer, Petropolis, RJ, Brazil) with copious irrigation using NaOCl 2,5% all teeth. The working length was established at approximately 1mm short of the radiographic apex, which was confirmed by periapical radiograph. The apical preparation was standardized using #40 K-files. The final irrigation of the root canals was performed with 5 ml of ethylenediaminetetraacetic acid 17%  (EDTA, Formula e Ação™, São Paulo, SP, Brasil), followed by 5ml of NaOCl 2,5% solution all teeth. Next, root canals were dried with the aid of absorbent paper points. Root canal filling was perfomed using gutta-percha points (Dentsply™, Maillefer, Petropolis, RJ, Brazil) compatible to the final file diameter (size #40) and endodontic cement (AH Plus™, Dentsply™, Constança, DE, Germany) without lateral compactation.

### All teeth received only 2 layers of ethyl cyanoacrylate (Henkel™ Ltd., São Paulo, SP, Brazil), applied with 60 seconds interval between each layer, on all root extension, to avoid dye external leakage. Then, the teeth were randomly divided into three experimental groups, as follows:

### -Group I (n=14):  the teeth were sealed with a layer of temporary restorative material (Cimpat Blanc™, Septodont™, Saint-Maurdes, FR, France) without intraradicular preparation (control group).

### -Group II (n=14): after intraradicular post preparation, the teeth were sealed with a layer of temporary restorative material (Cimpat Blanc™, Septodont™, Saint-Maurdes, FR, France).

### -Group III (n=14): after intraradicular post preparation, two layers of ethyl cyanoacrylate with 60 seconds interval between each one, and the teeth were sealed with a layer of temporary restorative material (Cimpat Blanc™, Septodont™, Saint-Maurdes, FR, France).

The teeth were weighed on precision scale, using the double sampling method, to establish the initial weight (IW). Then, the teeth were immersed into test tubes with Rhodamine B 1 % (Interlab™, São Paulo, SP, Brazil) and maintained in a dry kiln at 37ºC and 100% relative humidity for 48 hours. Following, the roots were washed with running water to remove any excess of dye and dried with absorbent paper sheet. The teeth were weighed again, using the double sampling method, to establish the final weight (FW). For each group, the formula FW - IW determined the dye-infiltrated weight. FW-IW values were then transformed into volume using the formula V=W/D, where D is Rhodamine B 1%  density (d=1.0657).

RESULTS

To analyze the difference between final and initial weight of the sample, paired t test was performed, the variable analysis, which showed no statistical difference between the initial and final weight (p <0.05) (Fig. 1). To analyze infiltration of the colorant, the volume was the comparison variable. Shapiro Wilk- test was applied and showed normal distribution of the variables. ANOVA (p = 0.0013 / p < 5 %) was also applied and determined a statistical difference between the groups. To check which groups differed from each other, Tukey test was applied (Fig. 2)

It was observed that Group I infiltrated a smaller amount of Rhodamine B 1% as compared to group II. Group III (internally waterproofed with ethyl cyanoacrylate) showed the smallest leakage rate when compared with the other groups, being statistically different (p < 0.05).

DISCUSSION

Microleakage is the passage of bacteria, fluid, and chemicals to the root canal3. If the temporary restorative material used between endodontic treatment sessions does not provide the hermetic sealing of the cavity, bacteria can reach the root canal affecting the desinfection obtained in the previous sessions of the treatment. These materials when subjected to leakage tests were susceptible to recontamination and likely to increase the failure rate between sessions during the treatment [3,6,10,15,16]. The requirement of provisional restorative materials is to provide an effective and durable seal between sessions of the root treatment.

However, the efficiency of temporary restorative materials is widely discussed and the literature reaches consensus that none is capable of sealing thoroughly [2,20]. To minimize microleakage, researchers have used ethyl cyanoacrylate to promote a waterproofing layer [21-23].

### The use of cyanoacrylate is efficient in preventing microleakage [21-24], specifically on teeth requiring prosthetic reconstruction, i.e., teeth demanding more than one appointment to be treated. Some studies reported that cyanoacrylate can be safely used in Medicine and Dentistry. In this study, the ethyl cyanoacrylate was used because it adheres to the dentin walls providing the inner sealing the conduct and our results showed that the group sealed with this adhesive was statistically better in preventing microleakage of Rhodamine B 1% when compared with the groups without waterproofing, accepting the hypothesis of this study

However, after its application a thick film of adhesive is formed inside the root canal. Although this formed film will not interfere with the prosthesis adaptation , since the flue molding is performed after the sealing. The use of dyes such as methylene blue, eosin, and Rhodamine B 1% are often used for infiltration analysis of restorative materials and this methodology is widely used for studies with this purpose, besides the facility of reproducing it [13-15].

This study used Rhodamine B 1% as it has small particle size, better penetration, water solubility, diffusability, and hard tissue nonreactivity [25,26].  The temporary restorative material (Cimpat™) used in this study is made of zinc oxide and zinc sulfate. The use of these substances in restorative materials is excellent because of the masticatory resistance to compression and abrasion. However, temporary restorative materials do not have good marginal sealing ability, favoring microleakage, which justifies the use of a waterproofing agent.

### In this study, the group subjected to intraradicular preparation without internal waterproofing (Group II) showed the highest dye-infiltrated weight and volume, while the group which was waterproofed with ethyl cyanoacrylate (Group III) showed the lowest dye-infiltrated weight and volume. The results of this study corroborate the literature by emphasizing that sealing with only temporary restorative material is not enough to avoid microleakage in endodontically treated teeth [5,6,9.13].

CONCLUSION

It can be concluded that the use of ethyl cyanoacrylate as internal waterproofing agent after intraradicular post preparation prevented Rhodamine B 1% microleakage.

REFERENCES

- Saberi E, Akbari N , Ebrahimipour S , Jalilpour H . In-vitro evaluation of coronal microbial leakage after post space tooth preparation. Minerva Stomatol. 2016;(3):65:127-133.

- Arora SJ, Arora A, Upadhyaya V, Jain S. Comparative evaluation of marginal leakage of provisional crowns cemented with different temporary luting cements: In vitro study. J Indian Prosthodont Soc. 2016;16(1):42-48.

- Prado M, Simão RA, Gomes BP. A microleakage study of gutta-percha/AH Plus and Resilon/Real self-etch systems after different irrigation protocols. J Appl Oral Sci. 2014;22(3):174-9.

- Heling I, Gorfil C, Slutzky H, Kopolovic K, Zalkind M, Slutzky-Goldberg I. Endodontic failure caused by inadequate restorative procedures: review and treatment recommendations. J Prosthet Dent. 2002;87(6):674-8.

- Khayat A, Lee SJ, Torabinejad M. Human saliva penetration of coronally unsealed obturated root canals. J Endod. 1993;19(9):458-461.

- Ray HA, Trope M. Periapical status of endodontically treated teeth in relation to the technical quality of the root filling and the coronal restoration. Int Endod J. 1995;28(1):12-8.

- Zaia AA, Nakagawa R, De Quadros I, et al. An in vitro evaluation of four materials as barriers to coronal microleakage in root-filledteeth. Int Endod J. 2002;35(9):729-734.

- Jensen AL, Abbott PV, Castro Salgado J. Interim and temporary restoration of teeth during endodontic treatment. Aust Dent J. 2007;52(1):83-99.

- Lai YY, Pai L, Chen CP. Marginal leakage of different temporary restorations in standardized complex endodontic access preparations. J Endod. 2007;33(7):875-8.

- Malone KHIII, Donelly JC. An in vitro evaluation of coronal microleakage in obturated root canals without coronal restorations. J Endod. 1997;23(1):35-8.

- Okida RC, Martins TM, Briso AL. In vitro evaluation of marginal leakage in bonded restorations, with mechanical or chemical-mechanical (Carisolv) removal of carious tissue. Braz Oral Res. 2007;21(2):176-81.

- Srikumar GPV. , Varma KR, Shetty HK, Kumar P. Coronal microleakage with five different temporary restorative materials following walking bleach technique: An ex-vivo study. Contemp Clin Dent. 2012;3(4):421-426.

- Cruz EV, Shigetani Y, Ishikawa K, Kota K, Iwaku M, Goodis HE. A laboratory study of coronal microleakage using four temporary restorative materials. Int Endod J. 2002;35(4):315-20.

- Oddoni PG, Mello I, Coil JM, Antoniazzi JH. Coronal and apical leakage analysis of two different root canal obturation systems. Braz Oral Res. 2008;22(3):211-5.

- Bönecker-Valverde G, Maniglia-Ferreira C, Abi-Rached GP, Gomes BP, Mesquita MF. Seal capability of interim post and core crown with temporary cements. Braz Oral Res. 2010;24(2):238-44.

- Zhang C, Hou BX, Zhao HY, Sun Z. Microbial diversity in failed endodontic root-filled teeth. Chin Med J. 2012;125(6):1163-8.

- Herod EL. Cyanoacrylates in dentistry: a review of the literature. J Can Dent Assoc. 1990;56(4):331-4.

- Montanaro L, Arciola CR, Cenni E, et al. Cytotoxicity, blood compatibility and antimicrobial activity of two cyanoacrylate glues for surgical use. Biomaterials. 2001;22(1):59-66.

- Guzman-Armstrong S, Mitchell RJ. Surface coating and leakage of dentin-bonded resin composite restorations. J Dent. 2002;30(2):113-8.

- Eliyas S, Jalili J, Martin N. Restoration of the root canal treated tooth. Br Dent J. 2015;218:(2):53-62.

- Jacobsen EL, Shugars KA. The sealing efficacy of a zinc oxide-eugenol cement, a cyanoacrylate and a cavity varnish used as root canal cements. J Endod. 1990;16(11):516-9.

- Wolanek GA, Loushine RJ, Weller RNW, Kimbrough F, Volkmann KR. In vitro bacterial penetration of endodontically treated teeth coronally sealed with a dentin bonding agent. J Endod. 2001;27(5):354-7..

- Holland R, Murata SS, Silva MN, Dezan Junior E, Souza Vd, Bernabé PF. Influence of the sealer and a plug in coronal leakage after post space preparation. J Appl Oral Sci. 2004;12(3):223-6.

- Chaves FD, Pécora JD, Silva RG. The effect on coronal leakage of liquid adhesive application over root fillings after smear layer removal with EDTA or Er: YAG laser. Oral Surg Oral Med Oral Pathol Oral Radiol Endod. 2005;99(2):125-128.

- Wu MK, Wesselink PR. Endodontic leakage studies reconsidered. Part I. Methodology, application and relevance. Int Endod J. 1993;26(1):37-43.

- Parekh B, Irani RS, Sathe S, Hegde V. Intraorifice sealing ability of different materials in endodontically treated teeth: An in vitro study. J Conserv Dent 2014;17(3):234-237.