**Table 2:** Mean and standard deviations of ART Class II restorations with and without proximal retentions (Kgf).

|  |  |  |
| --- | --- | --- |
| Restorative Material | Without retention | With retention |
| ChemFil Rock: | 300.84(69.20) A | 361.70(81.08) B |
| Equia Fil | 314.60(69.97) A | 366.67(103.38) B |

The results designated with the same letter are not statistically different (*p*<0.05).