Tables and Figures

| Groups (n=10) | Light Curing Unit | Technique |
| --- | --- | --- |
| HD | Halogen | direct |
| LD | Led | direct |
| HI | Halogen | direct-indirect |
| LI | Led | direct-indirect |

Table 1: The groups were divided according to the method and light polymerizing appliance used. The endodontically treated teeth were randomly divided into 4 groups with 10 samples in each.

| Group | Mean (N) | Standard Deviation |
| --- | --- | --- |
| HD | 142,30 | (±25,60)a |
| LD | 178,56 | (±25,67)b |
| HI | 246,05 | (±29,51)c |
| LI | 241,60 | (±28,95)c |

Table 2:  Different Letters (a,b,c,d) indicate  statistical differences among the groups based on ANOVA

Figure 1: Shows the mean of each group with its respective standard deviation

| Group | Resin/Dentin | Dowel/Resin | Mix |
| --- | --- | --- | --- |
| HD | 8 | 0 | 2 |
| LD | 10 | 0 | 0 |
| HI | 9 | 0 | 1 |
| LI | 10 | 0 | 0 |

Table 3: Fracture Classification after the Retention Test

Figure  2 - Failure occurred at the  resin/dentin interface

Figure  3 – Mixed Failure (resin/dentin and resin/dowel)