Figure 1. Control: gutta-percha points immersed for periods reported in the literature for each solution and without disinfection

Figure 2. Time of immersion of the gutta-percha points in the disinfectant

Figure 3.  Aspect of the surface morphology of gutta-percha points at 500x (A) and 5000x (B) magnification

Figure 4. Group (G1): control - gutta-percha points without disinfection (A); immersed in 1% NaOCl for 20 min (B) and immersed in 2.5% NaOCl for 10 min (C).

Figure 5. Group (G2): points immersed in 1% NaOCl for 30 minutes (A), 6 (B), 12 (C) and 24 hours (D).

Figure 6. Group G3: points immersed in 2.5% NaOCl for 30 minutes (A), 6 (B), 12 (C) and 24 hours (D).

Figure 7. Obtained images of the control group 1% NaOCl 20 minutes (A) and 2.5% NaOCl 10 minutes (B).Obtained images of the groups 1% NaOCl 30 min (C) and 24 hours (D). Obtained images of the groups 2.5% NaOCl 30 min (E) and 24 hours (F).

Figure 8. Graphic column (mean standard deviation) of the degree of dye penetration (mm) obtained in the roots sealed, under the experimental conditions established: concentration of sodium hypochlorite (1% and 2,5%) and disinfection time (30 min and 24 hours) and the two controls.

# Text boxes

G1 controle

30 gutta-percha points

10 points disinfection with NaOCl 2,5%    10min

10 points disinfection with  NaOCl 1%    20min

10 points        without           disinfection

G2                      G3

(NaOCl 1%)    (NaOCl 2,5%)

G2d /G3d G3d

G2c /G3c G3cG3c

G2b /G3b G3bG3b

G2a /G3a G3a

06h

12h

30 min

24h

B

##### A

##### A

##### C

##### B

##### A

##### B

##### C

##### D

##### D

##### C

##### B

##### A

##### E

##### b

##### A

##### B

##### D

##### C

##### F