Chart 1

| Groups | Name/ Manufacturer | Composition | References |
| --- | --- | --- | --- |
| G1(Control) | Without reinforcement | - | - |
| G2 | 0.7 mm metal orthodontic wires from Dental Morelli São Paulo-Brazil | Stainless steel | Ref. No. 55.01.070 Lot No. 352368 |
| G3 | Fibrex-lab® Angelus® Odonto Lógika Ind. Ltda, Londrina, PR – Brazil | Unidirectional glass fibers impregnated with resin composite | Ref. No. 471 Lot No. 11262 |
| G4 | Perma-Fiber® Angelus® Odonto Lógika Ind. Ltda, Londrina,PR – Brazil | Unidirectional glass fibers | Ref. No. 484 Lot No. 1183 |

Chart 1 – Description of the reinforcing material used and division of the groups

Table 1

Table 1 – Mean Flexural Resistance  (MPa) and standard deviation  (SD) for each group

|  | Group 1 | Group 2 | Group 3 | Group 4 |
| --- | --- | --- | --- | --- |
| Mean S.D. | 80.60 6.14 | 95.96 7.57 | 105.70 6.98 | 108.70 6.45 |

Table 2

Table 2 – Tukey Test for flexural resistance values (MPa) for four groups

| Harmonic Mean of number of repetitions (r): 10 Standard-Error 2.6775337999734 |
| --- |
| Treatments | Means | Test Results |
| 1 2 3 4 | 80.60 95.96 105.70 108.69 | A B BC C |

* different capital letters in the groups demonstrate significant differences at the level of 95%, repetitions of letters demonstrate that there was no statistical difference among the groups.