Original Article

Effect of root perforations on the bond strength of fiberglass post using different adhesive systems and resin cement

Claudio Hideki KUBO1,  Paloma Grasso MADUREIRA2,  Eduardo Galera da SILVA3,  Frederico Canato MARTINHO4,  Ana Paula Martins GOMES5,  Clóvis PAGANI5

1 PhD, Department of Restorative Dentistry, Institute of Science and Technology, UNESP – Univ Estadual Paulista, School of Dentistry, São José dos Campos, SP, Brazil.

2 Graduate Student, Department of Restorative Dentistry, Institute of Science and Technology, UNESP – Univ Estadual Paulista, School of Dentistry, São José dos Campos, SP, Brazil.

3 Assistant Professor, Department of Social and Pediatric Dentistry, Institute of Science and Technology, UNESP – Univ Estadual Paulista, School of Dentistry, São José dos Campos, SP, Brazil.

4 Assistant Professor, Department of Restorative Dentistry, Institute of Science and Technology, UNESP - Univ Estadual Paulista, School of Dentistry, São José dos Campos, SP, Brazil.

5 Associate Professor, Department of Restorative Dentistry, Institute of Science and Technology, UNESP - Univ Estadual Paulista, School of Dentistry, São José dos Campos, SP, Brazil.

Corresponding author:

Ana Paula Martins Gomes

Institute of Science and Technology

Avenida Engenheiro Francisco José Longo, 777, Jardim São Dimas

São José dos Campos, SP, Brasil, CEP 12245-000

e-mail:  paula@fosjc.unesp.br