Table 2. Specifications and procedures for the adhesive systems used

| Specifications | ClearFil SE Bond, Kuraray, Japan | Adper Single Bond 2, 3M/ESPE, St. Paul, MN, USA |
| --- | --- | --- |
| Composition | Self-etching primer: 10-MDP, HEMA, hydrophilic dimethacrylate, di camphorquinone, N,N-diethanol-p-toluidine, water Adhesive resin: MDP, Bis-GMA, HEMA, hydrophobic dimethacrylate, di-camphorquinone, N,N-diethanol-p-toluidine, silanized colloidal silica | Adhesive resin: water, alcohol, HEMA, BisGMA, dimethacrylate, copolymers of polyacrylic acids and acid polyitaconic |
| Procedures | First step: self-etching primer application on dentin for 20 seconds and gently air-dried Second step: adhesive resin application; air thinned and light polymerized for 10 seconds | First Step: etchant (35% phosphoric acid—3M/ ESPE) for 15 seconds and rinsed with water for 10 seconds Second step: application of two coats of Adper Single Bond 2 adhesive, the surface being gently air-dried for 5 seconds and light polymerized for 10 seconds |