Table 1 – Description of manufacturers, modes of application, composition and batch numbers of the cements.

| # Materials # (Manufacturer) | # Mode/Steps of application | # Composition | # Batch # |
| --- | --- | --- | --- |
| Enforce (Enforce; Dentsply, Petropolis, RJ, Brazil) | 1) Apply 35% phosphoric acid for 15s, using a light scrubbing motion 2) Rinse thoroughly and gently dry with with air and paper points 3) Apply adhesive (Prime & Bond 2.1 + Self Cure), then dried with air and polymerize for 40s by placing the light source on the top of post-space 4) Apply the cement onto the posts’ surfaces. 5) Insert and light cure for 40s | BisGMA, EBPADM, TEGDMA, butylhydoxitoluol, benzoyl peroxide, barium glass, silica | Catalyst 305390 |
|  |  |  | Base paste 305390 |
| RelyX Luting (3M ESPE, St. Paul, MN, USA). | 1) Etch the post space with polyacrylic acid for 15s 2) Rinse with water for 10s and dry with air and paper points 3) Apply the cement onto the posts’ surfaces and insert the post. | Powder: fluoroaluminosilicate glass, potassium persulfate, ascorbic acid catalyst system, opacifying agent | 5CX |
|  |  | Liquid: water, polycarboxylic acid, methacrylate groups, HEMA , tartaric acid | 5MP |
| RelyX Unicem (3M ESPE, Seefeld, Germany) | 1) Rinse the post space with water for 10s 2) Dry with air and paper points 3) Activate the capsule and mix the cement into a mixer for 15s 4) Apply the cement onto the posts’ surfaces. 5) Insert and light cure for 60s | Phosphoric acid methacrylates, dimethacrylates, inorganic fillers (72wt.%), fumed silica, initiators | 232722 |

* According to manufacturers information